## Slide 1
Ch.2 Parameter Extraction in
Time-Domain Spectrometers
Lee Jong Geon

## Slide 2
Material Properites and Wave Propagation
Extracting Optical Parameters fromTerahertz Time-Domain Spectromerters Data
Preprocessing and Postprocessing of Data
Sample Requirements
Contents

## Slide 3
Material Properties and
Wave Propagation

## Slide 4
1.1 Complex Refeactive Index and Complex Permitivity
Complex Refractive Index
Complex Permittivity Index
Kramers-Kronig relations

## Slide 5
1.2 Plane Wave Propagation Across an Interface – Fresnel Equations

## Slide 6
1.3 Plane Wave Propagation Through a Dielectric Slab

## Slide 7
1.4 Fabry-Pérot Effect

## Slide 8
Extracting Optical Parameters from
Terahertz TDS Data

## Slide 9
2.1 Transmission-Mode Terahertz TDS: Approximation
Dielectric slab at normal incidence

## Slide 10
2.2 Transmission-Mode Terahertz TDS: Exact Solution
It is based on minimizing error in the magnitude and phase components of the modeled transfer function with respect th the measured transfer function
Gradient-Descent Algorithm
Step 1: Estimate a range of possible thickness
Step 2: Initialize the complex refractive index
Step 3: Determine the modeled transfer function
Step 4: Estimate the error
Step 5: Update the complex refractive index
Step 6: Determine the total variation
Dorney, T., R. Baraniuk, and D. Mittleman, “Material Parameter Estimation with Terahertz Time-Domain Spectroscopy,” Journal of the Optical Society of America A: Optics, Image Science, and Vision, Vol. 18, No. 7, 2001.

## Slide 11
2.3 Reflection-Mode Terahertz TDS: Single Reflection
Single reflection  Two scan (reference, sample)
Double reflection  One scan (combined)
Gatesman, A. J., R. H. Giles, and J. Waldman, “High-Precision Reflectometer for Submillimeter wavelength,” Journal of the Optical Society of America B: Optical Physics, Vol. 12, No. 2, 1995.
Mirror and sample positioning become cruical

## Slide 12
2.4 Reflection-Mode Terahertz TDS: Double Reflection

## Slide 13
2.5 Attenuated Total Reflection
Møller, U., et al., “Terahertz Reflection Spectroscopy of Debye Relaxation in Polar Liquids,” JOSA B, Vol. 26, No. 9, 2009.
Nagai, M.m et al, “Terahertz Time-Domain Attenuated Total Reflection Spectroscopy in Water and Biological Solution,” International Journal of Infrared and Millimeter Waves, Vol. 27, No. 4, 2006.

## Slide 14
Preprocessing and
Postprocessing of Data

## Slide 15
3.1 Signal Averaging in the Time and Frequency Domains
Fischer, B. M., M. Hoffmann, and P. U. Jepsen, “Dynamic Range and Numerical Error Propagation in Terahertz Time-Domain Spectroscopy,” in Optical Terahertz Science and Technology, Technical Digest (CD). Optical Society of America, 2005, paper TuD1.
The averaging is effective in the time domain, but not in the frequency domain

## Slide 16
3.2 Signal Denoising
Fischer, B. M., M. Hoffmann, and P. U. Jepsen, “Dynamic Range and Numerical Error Propagation in Terahertz Time-Domain Spectroscopy,” in Optical Terahertz Science and Technology, Technical Digest (CD). Optical Society of America, 2005, paper TuD1.
Noise in a terahertz signal could be reduced by digital signal processing techniques in addition to signal averaging.

## Slide 17
3.3 Phase Unwrapping
Fischer, B. M., M. Hoffmann, and P. U. Jepsen, “Dynamic Range and Numerical Error Propagation in Terahertz Time-Domain Spectroscopy,” in Optical Terahertz Science and Technology, Technical Digest (CD). Optical Society of America, 2005, paper TuD1.
In most case the assumption of a linear phase is sufficient. Phase-jumping causes discontinuities in a phase spectrum

## Slide 18
Sample Requirements

## Slide 19
References
Dorney, T., R. Baraniuk, and D. Mittleman, “Material Parameter Estimation with Terahertz Time-Domain Spectroscopy,” Journal of the Optical Society of America A: Optics, Image Science, and Vision, Vol. 18, No. 7, 2001, pp. 1562-1571.
Gatesman, A. J., R. H. Giles, and J. Waldman, “High-Precision Reflectometer for Submillimeter wavelength,” Journal of the Optical Society of America B: Optical Physics, Vol. 12, No. 2, 1995, pp. 212-219.
Møller, U., et al., “Terahertz Reflection Spectroscopy of Debye Relaxation in Polar Liquids,” JOSA B, Vol. 26, No. 9, 2009, pp. A113-A125.
Nagai, M.m et al, “Terahertz Time-Domain Attenuated Total Reflection Spectroscopy in Water and Biological Solution,” International Journal of Infrared and Millimeter Waves, Vol. 27, No. 4, 2006, pp. 505-515.
Fischer, B. M., M. Hoffmann, and P. U. Jepsen, “Dynamic Range and Numerical Error Propagation in Terahertz Time-Domain Spectroscopy,” in Optical Terahertz Science and Technology, Technical Digest (CD). Optical Society of America, 2005, paper TuD1.