## Slide 1
20181217
Tungsten Tip Etching
-paper review-
Lee Jong Geon

## Slide 2
2002-Nano Letters-2,3-Reproducible Electrochemical Etching of Tungsten Probe Tips (Olivier L. Guise, Joachim W. Ahner, Moon-Chul Jung, Peter C. Goughnour, and John T. Yates, Jr.)
Post-etching: wire가 끊어진 이후에도 etching process를 진행하는 것
An average of at least 5 tips.
“This method produces tips in a very controlled and reproducible manner.”
Two step etching
Coarse etching: 2M KOH, DC 3V
post etching: 0.1M KOH, DC 0.5 V
Switch: 500 ns

## Slide 3
2012-Rev. Sci. Instrum.-83,6-Two step controllable electrochemical etching of tungsten scanning probe microscopy tips(Yasser Khan, Hisham Al-Falih, Yaping Zhang, Tien Khee Ng, Boon S. Ooi)
325 μm/s proved to give a stable etching voltage
One-step etching : RoC < 40 nm, ∼80% success rate
Two-step etching: RoC < 10 nm, ∼90% success rate

## Slide 4
2017-Microelectronic Engineering-173-Progrmmable set-up for electrochemical preparation of STM tips and ultra-sharp field emission cathods(Alexandr Knapek, jiri Sykora, Jana Chlumska, Dinara Sobola)
“The programming allows for increasing the reproducibility of the preparation and improves the quality of the preparation process.”
etching voltage: 6.9 V
current limit: 20mA
* both the one-step and two-step

## Slide 5
1978-J. Phys. D: Appl. Phys.-11-A comparison of AC and DC electrochemical etching techniques for the fabrication of tungsten whiskers (G. J. Edwards and P. R. Pearce)
AC
DC
Conical shape
AC etching: vigorous bubbling -> not affect the shape
DC etching: few bubbles -> irregular tip shapes

## Slide 6
2018-Micro&Nano Letters-13,8-Electrochemical etching of lightweight nanotips for high quality-factor quartz tuning fork force sensor: atomic force microscopy applications (Danish Hussain, Jianmin Song, Hao Zhang, Xianghe meng and Hui Xie)
Two step
Primary shaft diameter: 10–40 μm
Length: 2–5 mm
Fabricated with high success rate (∼80%).
High Q-factor
20 Hz

## Slide 7
10M
2012-Rev. Sci. Instrum.-83,08374-Method of electrochemical etching of tungsten tips with controllable profiles(Wei-Tse Chang, Ing-Shouh Hwang, Mu-Tung Chang, Chung-Yueh Lin, Wei-Hao Hsu and Jin-Long Hou)
DC(uniform)
etching
Pulse
etching
“we propose a simple and reliable electrochemical method to fabricate tungsten tips with good control of the tip profile.”

## Slide 8
2010-Journal of The Electrochemical Society-157,1-Optimization of AC Electrochemical etching for Fabricating Tungsten Nanotips with Controlled Tip Profile (S. L. Toh, H. Tan, J. C. Lam, C. Hsia, Z. H. Mai)
AC power supply: 13.5 V, 50 Hz
-> variable resistor selected(1.8 ~ 5.2 V)
0.5 M KOH
0.5 M KOH, 3.2 V