## Slide 1
Compound | Zero-field splitting (cm-1) | Excitation | Ref.
 | ΔEⅢ, Ⅰ |  | 
Pt(4,6-dFppy)(acac) | 8 (0.24 THz) | 335 nm | [1]
Pt(thpy)2 | 16 (0.48 THz) | 337.1 nm | [2]
Pt(dphpy)(CO) | 17.5 (0.52 THz) | 337.1 nm | [3]
Pt(Me4-salen) | 20 (0.6 THz) | 355 nm | [4]
Ir(btp)2(acac) | 25 (0.75 THz) | 373, 488, 514.5 nm | [5]
Pt(ph-salen) | 28 (0.84 THz) |  | 
Pt(ppy)2 | 32 (0.96 THz) |  | 
Pt(bhq)2 | 39 (1.17 THz) |  | 
Re(phen)(CO)3(Cl) | 42 (1.26 THz) |  | 
[Ru(bpy)3]2+ | 63 (1.89 THz) |  | 
[Os(phen)2{dppee)]2+ | 64 (1.92 THz) |  | 
Ir(4,6-dFppy)2(pic) | 76 (2.28 THz) |  | 
Ir(ppy)3 | 83.5 (2.5 THz) |  | 

## Slide 2
[1] Rausch, A. F., Thompson, M. E., & Yersin, H. (2009). Triplet state relaxation processes of the OLED emitter Pt (4, 6-dFppy)(acac). Chemical Physics Letters, 468(1-3), 46-51.
[2] Yersin, H., Schützenmeier, S., Wiedenhofer, H., & Von Zelewsky, A. (1993). Highly resolved optical spectra of palladium complex with deprotonated 2-(2-thienyl) pyridine (Pd (2-thpy) 2) in a Shpol'skii matrix. The Journal of Physical Chemistry, 97(51), 13496-13499.
[3] Kratzer, Cornelius (2005) Hochauflösende optische Spektroskopie am Pt(dphpy)(CO)-Triplett-Emitter und Untersuchungen zum Energietransfer in einem quasi-zweidimensionalen Tb[Au(CN)2]3 · 3 H2O-Halbleiter. PhD, Universität Regensburg.
[4] Che, C. , Kwok, C. , Lai, S. , Rausch, A. , Finkenzeller, W. , Zhu, N. and Yersin, H. (2010), Photophysical Properties and OLED Applications of Phosphorescent Platinum(II) Schiff Base Complexes. Chemistry – A European Journal, 16: 233-247. doi:10.1002/chem.200902183
[5] Triplet State Properties of the OLED Emitter Ir(btp)2(acac): Characterization by Site-Selective Spectroscopy and Application of High Magnetic Fields, Walter J. Finkenzeller,†, Thomas Hofbeck,†, Mark E. Thompson,‡ and, and Hartmut Yersin*,†, Inorganic Chemistry 2007 46 (12), 5076-5083, DOI: 10.1021/ic0622860